line x location= 0.0      spacing= 1.0<nm>  tag= SiTop

line x location= @depth@<um> spacing= 1.0<um>  tag= SiBottom

line y location= 0.0      spacing= 250<nm>  tag= left

line y location= @length@<um> spacing= 250<nm>  tag= Right

#------mesh definition----------

region Silicon xlo= SiTop xhi= SiBottom ylo= left yhi= Right

init concentration= 1e15<cm-3> field= Phosphorus !DelayFullD

#------wafer initialization--------

gas_flow clear

gas_flow name= flow1 pressure= 1.0<atm> flowO2= 0.1<l/min> flowN2= 10.0<l/min>

gas_flow name= flow2           pressure= 1.0<atm> flowO2= 1.0<l/min>

temp_ramp name= PadOxide clear

temp_ramp name= PadOxide time= (1050.0-700.0)/75<s> temperature= 700.0<C> ramprate= 75<K/s>  gas.flow= flow1

temp_ramp name= PadOxide time= 1.5<min> temperature= 1050.0<C>   gas.flow= flow2

temp_ramp name= PadOxide time= (1050.0-700.0)/20<s> temperature= 1050.0<C> ramprate= -20<K/s> gas.flow= flow1

diffuse temp.ramp= PadOxide

#diffuse temperature = 1000 time = 1<min> O2

#------------pad oxide--------------

deposit Nitride isotropic thickness= 0.2

#------------nitride formation-------

set TrenchLeftCoord   0.125

set TrenchRightCoord  1.375

mask name= STI  segments= { 0 $TrenchLeftCoord $TrenchRightCoord 1.5}

photo mask= STI thickness= 0.5

etch Nitride anisotropic thickness= 0.2*1.5

etch Oxide anisotropic thickness= 0.2*1.5

strip      Photoresist

set TrenchAngle 88.0

set TrenchDepth 3.5

etch Silicon type= trapezoidal thickness= $TrenchDepth angle= $TrenchAngle

gas_flow clear

gas_flow name= H2O  pressure= 1.0<atm> flowH2O= 1.0<l/min>

temp_ramp name= Liner_Oxide clear

temp_ramp name= Liner_Oxide time= 0.25<min> temperature= 1050.0<C> gas.flow= H2O

diffuse temp.ramp= Liner_Oxide

deposit Oxide isotropic thickness= 4.5

etch material= all  type= cmp  coord= 0.0065

deposit Oxide isotropic thickness= 0.01

##implant  Boron  dose= 2.0e13<cm-2>  energy= 180<keV> tilt= 7 rotation= 0

implant  Boron  dose= 1.0e13<cm-2>  energy= 50<keV> tilt= 7 rotation= 0

implant  Boron  dose= 5.0e12<cm-2>  energy= 20<keV> tilt= 7 rotation= 0

etch material= all  type= cmp  coord= 0.0065

diffuse temperature= 1050<C> time= 10.0<s>

deposit Oxide isotropic thickness= 10<nm>

set n_LeftCoord   0.9

set n_RightCoord  1.3

mask name= n_rgr  segments= {$n_LeftCoord $n_RightCoord }

photo mask= n_rgr  thickness= 0.4

implant  Arsenic  dose= 2.0e13<cm-2>  energy= 50<keV> tilt= 7 rotation= 0

diffuse temperature= 1000<C> time= 5.0<s>

strip photoresist

set p_LeftCoord   0.3

set p_RightCoord  .35

mask name= p_poc_rgr  segments= {$p_LeftCoord $p_RightCoord }

photo mask= p_poc_rgr thickness= 0.4

implant  Boron  dose= 5.0e13<cm-2>  energy= 5<keV> tilt= 7 rotation= 0

#####RTA-----------------

diffuse temperature= 950<C> time= 2.0<s>

etch material= Oxide type = anisotropic thickness= 0.05

strip photoresist

mask name= n_cnt  segments= {1 1.2 }

photo mask= n_cnt thickness= 0.4

etch material= Oxide type = anisotropic thickness= 0.05

strip photoresist

deposit Aluminium isotropic thickness= 75<nm>

mask  name= Cnt_Al segments = {0.28 0.37 0.88 1.32} negative

photo mask= Cnt_Al thickness= 40<nm>

etch material= Aluminium type= anisotropic thickness=80<nm>

strip photoresist

deposit Nitride isotropic thickness= 40<nm>

set p_LeftCoord   0.3

set p_RightCoord  .35

set n_LeftCoord   0.9

set n_RightCoord  1.3

mask name= mask3 segments= {$p_LeftCoord $p_RightCoord $n_LeftCoord $n_RightCoord}

photo mask= mask3 thickness= 0.3

etch  material= Nitride type= anisotropic thickness= 40<nm>

strip photoresist

## Contact placement

contact name= "anode" box Aluminium  xlo= -0.08 xhi= 0.01 ylo= 0.26 yhi= 0.38

contact name= "cathode" box Aluminium  xlo= -0.08 xhi= 0.01 ylo= 0.85 yhi= 1.35

line      clear

refinebox clear

refinebox name= Global    min= {0 0} max= {6 1.5} xrefine= 0.2 yrefine= 0.5

refinebox name= PN min= {0 0} max= {1 1.5} xrefine= 0.02 yrefine= 0.02

refinebox interface.mat.pairs= {Silicon Aluminium }

grid remesh

struct tdr = n@node@